## Slide 1
2024. 11. 14
Korea Atomic Energy Research Institute (KAERI)
Transient superhydrophilic surface modification of polyimide by metal ion beam irradiation
Sunmog Yeo
Langmuir (2024) 40, 12200-12206

## Slide 2
Experimental set up
Contents
2
1
Background
1
Results and discussion
3
Summary
4

## Slide 3
Background
@ Superhydrophilic surface
Superhydrophilic
Superhydrophobic
Superhydrophilic application
Funshop 제공
1) Self-Cleaning
2) Anti-fogging
3) Biomedical Application : implant materials
…. etc
4) Ink printing
ACS applied Materials and Interface. Vol 6 (2014) 4011
Patterned surface with controllable wettability for inkjet printing of flexible printed electronics
Notes: 열교환효율 향상  쿨링시스템 적용,

## Slide 4
Background
@ Flexible display panel substrate
Necessary condition for the flexible display substrate
Flexibility and durability
Excellent dimensional stability (humidity, temperature)
Lightweight
Transparency and optical properties (reflectivity, refractivity)
Electrical properties (Insulator, low permittivity)
Thermal stability (low thermal expansion coefficient)
Chemical stability (resistance for harsh chemical process)
etc..
What are the good canditators?
Polyimide (PI), Polyethylene Terephthalate (PET),
Polycarbonate (PC), Polymethyl methacrylate (PMMA)
Notes: 열교환효율 향상  쿨링시스템 적용,

## Slide 5
Background
@ Electrode formation processes on the flexible display substrate
PVD (Physicial Vapor Deposition) : E-Beam evaporation, sputtering
CVD (Chemical Vapor Deposition)
Inkjet printing, Screen Printing
(Cheap, easy  Industrial application)
etc..
In order to enhance adhesion between substrates and ink (or paste), surface treatments should be done, especially, superhydrophilic surface treatments.
Notes: 열교환효율 향상  쿨링시스템 적용,

## Slide 6
Background
  In order to make superhydrophilic surface of polyimide, various surface treatments have been applied such as chemical treatments, plasma treatments, etc.
  The chemical treatments, however, produces a lot of detrimental wastes to the environment.
@ Motivation
  Is there anyway to achieve superhydrophilic surface without detrimental wastes?
  Surface treatments by Ion beam irradiation are environmental friendly tools and generate no detrimental wastes

## Slide 7
Experimental set up
@ Ion implanter operated by KAERI (Korea Atomic Energy Research Institute)
Gas implanter
Ion source : DuoPIGatron
Energy range : 20 ~ 200 keV
Ion species : H+, He+, N+, O+, Ne+, Ar+, Kr+, etc.
Metal implanter
Ion source : Bernas type ion source
Energy range : 20 ~ 150 keV
Ion species : Mg+, Ti+, Cr+, Fe+, Co+, Ni, Cu+, etc.
양성자과학연구단 홈페이지 : www.komac.re.kr

## Slide 8
Experimental set up
Metal ion implanter
Burnace
ion source
Mass separation
magnet
Acceleration
tube
MQD
Scanner
Faraday cup
Target
Chamber
Energy : 20 ~ 140 keV
Peak current : ~ 1 mA
Irradiation area : ~ 100 mm-φ
Possible ion species :
Co, Fe, Cu, Cr, Mg, Ti, Ag etc

## Slide 9
Experimental set up
SEO (Model : Phonix-MTT)
@ Contact angle Measurement
For the contact angle measurements, we used a drop of water.

## Slide 10
Experimental set up
FTIR
Agilent (Model : Cary 660 IR)
Surface bonding characterization
@ Surface analysis equipment
Nano-indenter
CPX-UNHT
Surface hardness, elastic modulus
Surface morphology  AFM

## Slide 11
Results and discussion
@ SRIM simulation for metal ion beam irradiation (Cu+, Ti+)
Ion beam irradiation condition
Energy : 20 keV
Ion species : Cu+

## Slide 12
Results and discussion
@ SRIM simulation for metal ion beam irradiation (Cu+, Ti+)
Ion beam irradiation condition
Energy : 20 keV
Ion species : Ti+

## Slide 13
Results and discussion
@ Surface morphology change by metal ion beam irradiation (Cu+)
Change ion beam current density
(b)
0.5 μA/cm2
(c)
1.5 μA/cm2
(d)
2.0 μA/cm2
(a)
Pristine

## Slide 14
Results and discussion
@ Surface morphology change by metal ion beam irradiation (Ti+)
Change ion beam current density
(a)
0.3 μA/cm2
(b)
0.5 μA/cm2
(c)
0.7 μA/cm2
(d)
0.9 μA/cm2

## Slide 15
Results and discussion
@ Contact angle change by metal ion beam irradiation (Cu+)
current density : 0.5 μA/cm2.
Pristine PI
56.9o
4 min : 38.3o
6 min : 47.3o
12 min : 60.8o
60 min : 65.7o
3 h: 70.2o
8 day : 71.3o

## Slide 16
Results and discussion
@ Contact angle change by metal ion beam irradiation (Cu+)
current density : 1.0 μA/cm2.
Pristine PI
56.9o
4 min : 23.4o
6 min : 46.4o
16 min : 59.1o
60 min : 63.6o
1 day : 64.5o
8 day : 70.6o

## Slide 17
Results and discussion
@ Contact angle change by metal ion beam irradiation (Cu+)
current density : 1.5 μA/cm2.
Pristine PI
56.9o
4 min : 22.8o
6 min : 40.6o
16 min : 59.1o
3 h : 64.4o
1 day : 66.2o
8 day : 69.7o

## Slide 18
Results and discussion
@ Contact angle change by metal ion beam irradiation (Cu+)
current density : 2.0 μA/cm2.
Pristine PI
56.9o
4 min : 20.5o
6 min : 37.1o
16 min : 57.1o
3 h : 64.0o
1 day : 66.2o
8 day : 67.3o

## Slide 19
Results and discussion
@ Contact angle change by metal ion beam irradiation (Ti+)
current density : 1.3 μA/cm2.
Pristine PI
56.9o
5 min : 30.98o
12 min : 58.88o
30 min : 70.73o
0.5 μA/cm2: 64.1 o
0.7 μA/cm2 : 64.6 o
0.9 μA/cm2 : 68.7 o

## Slide 20
Results and discussion
@ Contact angle change by metal ion beam irradiation (Ti+)
Cu irradiation
● 0.5 μA/cm2
□ 1.0 μA/cm2
▲ 1.5 μA/cm2
○ 2.0 μA/cm2
Contact Angle (◦)
Contact Angle (◦)
Long time after Ti irradiation
Current density(μA/cm2)

## Slide 21
Results and discussion
@ Mechanical properties by metal ion beam irradiation
Current density(μA/cm2)
Surface Hardness (GPa)
Elastic Modulus (GPa)
Triangle : Cu
Circle : Ti.

## Slide 22
Cu 20 keV
J = 0.5 μA/cm2
2 min
4 min
6 min
8 min
12 min
Result and discussion
Absorbance FTIR Spectrum for polyimide
2 min
4 min
6 min
8 min
12 min
Large absorbance indicates that the specific bonds exists a lot in the materials.
For J = 0.5 μA/cm2, 2 min after irradiation displays the lower absorbance suggesting that the amount of C=O symmetric stretching bonds are small.
In other words, C=O bonds at 1720 cm-1 are restored by time.
C-N
Stretching
C=O
Symmetric stretching

## Slide 23
Results and discussion
@ FTIR spectrum analysis
Wavenumber (cm-1)
Absorbance (a. u)
C=O
Symmetric stretching
C-N
Stretching
2 min
4 min
6 min
8 min
12 min
pristine
Absorbance (a. u)
Absorbance peaks indicate the presence of corresponding vibration modes in materials.
Metal ion beam breaks some C=O symmetric stretching mode and C-N stretching mode.
The incomplete bonds cause the high surface energy which arise superhydrophilic surface.
Cu 20 keV
J = 2.0 μA/cm2

## Slide 24
Summary
Superhydrophilic surface is very useful to our lives.
Ion beam irradiation is an environmental friendly surface treatment tool so that the surface treatment for the polyimide is a good application materials.
By using ion beam irradiation, superhydrophilic surface of polyimide can be obtained.
The FTIR spectrum analysis reveals that ion beam irradiation produces high surface energy states by breaking C=O and C-N bond temporarily and the bonds are recovered after all.
Even though ion beam irradiation affects surface properties of polyimide, the mechanical properties of polyimide are similar.

## Slide 25
Thank you for your attention !!